Name: _________________________________			Date:__________________________

d e s i g n    o f   t h e    w e e k

# Space Shuttle Thermal Protection System: LI-900 Silica Insulation Tiles

On February 1, 2003, the Space Shuttle Columbia catastrophically disintegrated during reentry resulting in the loss of the space vehicle and the loss of life of all of the astronauts on board.  After an exhaustive investigation, it was found that the failure was caused by a breach in the thermal protection system.   The breach was caused by a large piece of insulating foam  that broke away from the external tank and impacted the leading edge of Columbia’s left wing during launch.

An excerpt from the official investigation details how the breach in Columbia’s left wing resulted in the ultimate loss of the space vehicle:

[The] conclusion is that Columbia re-entered Earthʼs atmosphere with a preexisting breach in the leading edge of its left wing in the vicinity of Reinforced Carbon-Carbon (RCC) panel 8. This breach, caused by the foam strike on ascent, was of sufficient size to allow superheated air (probably exceeding 5,000 degrees Fahrenheit) to penetrate the cavity behind the RCC panel. The breach widened, destroying the insulation protecting the wingʼs leading edge support structure, and the superheated air eventually melted the thin aluminum wing spar. Once in the interior, the superheated air began to destroy the left wing. This destructive process was carefully reconstructed from the recordings of hundreds of sensors inside the wing, and from analyses of the reactions of the flight control systems to the changes in aerodynamic forces.

Calculate the Heat Flux (W/in2) through a 2-inch thick section of LI-900 subject to a T of 2500 °C and compare it to the heat flux through a 0.25 inch thick section of steel subject to the same temperature difference.   The thermal conductivity of the LI-900 material is 0.048 W/m°C.  The thermal conductivity of steel is 40 W/m°C.

# Footnotes

Columbia Accident Investigation Board Report, Volume 1, August 2003